## Slide 1: Steam Methane Reformation For Air-Independent Solid Oxide Fuel Cells
Presenter: Kamwana Mwara

## Slide 2: HESTIA Architecture

## Slide 3: Why Steam Methane Reformation?
Background
  The availability of LOx/CH4 in the HESTIA-ISRU architecture, introduces Solid Oxide Fuel Cells (SOFCs) as an option, due to their ability to efficiently utilize those reactants.
Notes: 4 cylinder design:
  Based on SMR Matlab model which took into consideration:
    System & architecture constraints
    Desired methane reaction rates & equilibrium molar fractions
    Catalyst contact with steam & methane mixture
    Heat transfer rate to catalyst
    Length & area of SMR tubes
  Pros of 4 cylinder design:
    More catalyst contact with gas mixture
    Smaller diameter of tubes gives even more heating

## Slide 4: Why Steam Methane Reformation?
Introduction
  SOFCs can do internal reforming to convert CH4 into H2 to be used for fuel
    But would be optimal to reform methane externally first
  Utilizing an external steam methane reformer (SMR) would be the first step to creating a more efficient SOFC system
Notes: 4 cylinder design:
  Based on SMR Matlab model which took into consideration:
    System & architecture constraints
    Desired methane reaction rates & equilibrium molar fractions
    Catalyst contact with steam & methane mixture
    Heat transfer rate to catalyst
    Length & area of SMR tubes
  Pros of 4 cylinder design:
    More catalyst contact with gas mixture
    Smaller diameter of tubes gives even more heating

## Slide 5: HESTIA SMR Testing
Need:
  Obtain data on SMR CH4 conversion efficiencies and operating conditions, in support of HESTIA
Objective:
  To design, develop, & in-house SMR system
  Determine optimal operating conditions, reactor design, fluid delivery, & heating
  Utilize lessons learned from in-house testing, to generate requirements for vendor-provided SMR integration with SOFC
Phases of JSC In-House Testing:
  Phase 1: Test reactor design based off of theoretical Matlab model
  Phase 2: Test refined reactor and system design
  Phase 3: Test optimized system design and new metal foam catalyst
Notes: 4 cylinder design:
  Based on SMR Matlab model which took into consideration:
    System & architecture constraints
    Desired methane reaction rates & equilibrium molar fractions
    Catalyst contact with steam & methane mixture
    Heat transfer rate to catalyst
    Length & area of SMR tubes
  Pros of 4 cylinder design:
    More catalyst contact with gas mixture
    Smaller diameter of tubes gives even more heating

## Slide 6: SMR Testing: Phase 1
System Layout
Catalyst
Nickel Oxide Catalyst
Hot Flow Test (With Preheating of Gases) |  |  |  |  | 
Test # | CH₄ Mass Flow Rate [g/min] | H₂O Mass Flow Rate [g/min] | Steam to Methane Ratio [mol/mol] | SMR Temperature [˚F] | System Pressure [psia]
1 | 0.982 | 1.2 | 1 | 1020 | 14.7
2 | 0.982 | 2.3 | 2 | 1020 | 14.7
3 | 0.982 | 3.3 | 3 | 1020 | 14.7
Reasons for selection:
  Low cost
  Reasonably good efficiency
Notes: 4 cylinder design:
  Based on SMR Matlab model which took into consideration:
    System & architecture constraints
    Desired methane reaction rates & equilibrium molar fractions
    Catalyst contact with steam & methane mixture
    Heat transfer rate to catalyst
    Length & area of SMR tubes
  Pros of 4 cylinder design:
    More catalyst contact with gas mixture
    Smaller diameter of tubes gives even more heating

## Slide 7: SMR Testing: Phase 1
Generated H2 production, and also high build-up of upstream pressure

## Slide 8: SMR Testing: Phase 1
Test results:
  Initial production of Hydrogen
  Carbon deposition blockage in the catalyst bed
Conclusions:
  Use of a kiln to produce steam
  No steam flow regulation (steam-to-methane ratio)
  Catalyst was not reduced:
  𝑁𝑖𝑂+𝐻2↔𝑁𝑖+𝐻2𝑂
Phase 2 recommendations:
  Use syringe pumps to regulate water flow
  Use a separate heater to generate steam
  Reduce catalyst

## Slide 9: SMR Testing: Phase 2
System Layout
Improvements

## Slide 10: SMR Testing: Phase 2
Observed temperature and pressure transients – Affected H2 production at certain points

## Slide 11: SMR Testing: Phase 2
Test Results:
  Higher overall amount of hydrogen being produced
  Carbon deposition still being generated, though at lower rate
Conclusions:
  Catalyst was not sufficiently reduced
  Need to increase thermal mass to heat up fluids to design temperatures
  Need to minimize hotspots that promote carbon deposition
  Essential to maintain consistent heating profile for input stream going into the reactor
Recommendations:
  Obtain more robust catalyst
  Conduct one more round of testing, with system modifications
Carbon deposition in test system

## Slide 12: SMR Testing: Phase 3
System modifications:
  Switched to new metal foam catalyst – for increased chemical stability and potential conversion efficiency
Ordered Pd/Rh coated SIC metal foam catalyst, machined to SMR physical dimensions with through-hole for high temp temperature probe
Heat Transfer | Mass Transfer
Higher thermal conductivity minimizes temperature gradients & hot spots | Porous structure provides more tortuous path for gas molecules
Helps favor the reactions we want and prevent those we don’t | Better dispersion of the active metals coated on the metal foam structure

## Slide 13: SMR Testing: Phase 3
System modifications:
  Installed 3-way valve downstream of steam generator, to help avoid T and P transients (circled in green)
  Installed heating tape between steam generator and reactor, to maintain consistent heating profile (circled in red)

## Slide 14: SMR Testing: Phase 3
Initial test run – steadier temperature and pressure rates

## Slide 15: SMR Testing: Phase 3
Final test run – steady pressure flow, fluctuating H2 production

## Slide 16: SMR Testing: Phase 3 & Test Summary
Testing Results:
  Test prematurely ended due to leaking relief valve
  Eliminated carbon deposition
  Similar H2 conversion rates to Phase 2
Conclusions/Lessons Learned:
  Ensure relief valve has captured venting
  When possible, run higher flow rates in order to determine whether conversion efficiency increases
  Potentially better to use water flow controller instead of syringe pumps
SMR Overall Test:

## Slide 17: SMR Testing: Current Development
Goal:
  Private vendor SolidCell, Inc. to develop new SMR system
    Based on technical requirements and direction provided by JSC, generated by lessons learned from in-house testing
  SMR system to be integrated with existing JSC 1 kW SOFC system
Why:
  Develop more flight-like system, to include capacity for recirculation of SOFC product water and partial parasitic load capabilities
How:
  Test Conditions include:
    Water source: DI Water/SOFC Product water
    Operating Temperature ≥ 600oC
    Operating Pressure: 0-15 psig
    Steam-to-Methane Molar Mixture Ratio: ≥3

## Slide 18: SMR Testing: What’s Next
Testing:
  SMR System to be delivered at end of May
  Integration & testing with SOFC to happen by end of September (FY’16)
  Afterward, integrated testing with SOFC, CFM, and other ISRU architecture
    Use CH4 from CFM boiloff
Develop More Flight Ready Design:
  Recirculate product gases, along with H2O
  Enable SMR and supporting components act as a fully parasitic loads on SOFC
  Contain SMR & SOFC in same furnace